## Slide 1: Effective Strain Hardening Coefficient for Irradiated 9Cr ODS Alloy by Nano-Indentation and TEM
Corey Dolph1
1Wharry Group
Research Assistant
Boise State University

## Slide 2: OBJECTIVE
Demonstrate the ability to characterize plastic deformation in nano-grained alloys
Determine the effect of irradiation exposure on the tensile properties of a 9Cr ODS steel

## Slide 3: OVERVIEW
Background
  Oxide Dispersion Strengthened (ODS) Steel
  Irradiation Effects on Metals
  Nano-Indentation
Characterization of Plastic Zone
Changes in Tensile Properties

## Slide 4: BACKGROUND
Why the research interest in Oxide Dispersion Strengthened Steels?

## Slide 5: BACKGROUND
Oxide Dispersion Strengthened Steel
[1]

## Slide 6: BACKGROUND
Oxide Dispersion Strengthened Steel
Desire to develop future nuclear reactor designs that are:
  Safer
  More energy efficient
  Proliferation resistant

## Slide 7: BACKGROUND
Oxide Dispersion Strengthened Steel
Characteristics required for increased efficiency:
  Resistance to thermal and irradiation creep
  Adequate strength, ductility, and fatigue resistance
  Resistance to radiation damage
  Chemical stability

## Slide 8: BACKGROUND
Oxide Dispersion Strengthened Steel
Ferritic Martensitic Steels
[2]
[3]

## Slide 9: BACKGROUND
Oxide Dispersion Strengthened Steel
Ferritic Martensitic Steels
[2]
[3]
[4]

## Slide 10: BACKGROUND
Oxide Dispersion Strengthened Steel
Tensile properties of F-M steels break down at .
[5]

## Slide 11: BACKGROUND
Oxide Dispersion Strengthened Steel
[5]
Final Heat Treatments
1050°C x 1 h
800°C x 1 h
Effective grain diameter 230 nm

## Slide 12: BACKGROUND
Irradiation Effects
[6]

## Slide 13: BACKGROUND
Irradiation Effects
[6]

## Slide 14: BACKGROUND
Irradiation alters the microstructure:
  Point defects
  Precipitates
  Oxide Instability
  Chemical Segregation
Results in changes in material properties
Precipitates
Dislocation Network

## Slide 15: BACKGROUND
Irradiation Effects
[7]

## Slide 16: BACKGROUND
Uses
  Hardness
  Elastic modulus
  Strain hardening index
  Fracture toughness
  Yield strength
Specifications
  Two modes of Control
    Load
    Displacement
The Curve
  Loading
  Maximum Load
  Unloading
Error
  Creep
  Thermal Drift
  Surface Roughness
Nano-Indentation

## Slide 17: BACKGROUND
Johnson’s Model
Nano-Indentation
indentation depth
[8]

## Slide 18: Experimental APPROACH
Irradiate the Samples
Perform Nano-Indentation
Determine Plastic Zone
Determine Tensile Properties

## Slide 19: Experimental APPROACH
Irradiate the Samples
Perform Nano-Indentation
Determine Plastic Zone
Determine Tensile Properties
Three Test Conditions:
Ion Irradiated
Neutron Irradiated
As Received

## Slide 20: IRRADIATIONS
Ion Irradiated:
  Section Sample
    20mm x 2mm x 2mm bar
  Mechanically Polish
    Through 4000 grit SiC Paper
  Electropolish
    10% Perchloric acid
    90% Methanol
    20 seconds
    -40°C
    35 V
Neutron Irradiated:
  Section Sample
    3 mm discs
    150 – 200 μm thick
  Mechanically Polish
    Through 4000 grit SiC Paper
  Electropolish
    10% Perchloric acid
    90% Methanol
    -35°C
Sample Preparation

## Slide 21: IRRADIATIONS
Ion Irradiations:
  Michigan Ion Beam Laboratory
  5 MeV Fe++ Ions
  Dose: 100 displacements per atom (dpa)
    SRIM 2013™
    Detailed Calculation
    600 nm
    Layer Thickness = 1.94 μm
  Temp: 399.3 4.4°C
dpa
199
142
85
28
0
Depth (nm)
2000
600
100
1280
237

## Slide 22: IRRADIATIONS
Neutron Irradiations:
  Advanced Test Reactor (ATR) at Idaho National Lab
  Dose: 3 dpa
  Temp: 500°C
[9]

## Slide 23: Experimental APPROACH
Irradiate the Samples
Perform Nano-Indentation
Determine Plastic Zone
Determine Tensile Properties

## Slide 24: NANO-INDENTATION
As Received
  Section Sample
    Allied Techcut 4™ Diamond Saw
  Mechanically Polish
    Allied-M prep B™
    Through 1200 grit SiC Paper
    Buehler MetaDi™ Poly Crystalline Diamond Suspension through 0.05μm
  Electropolish
    10% Perchloric acid
    90% Methanol
    20 Seconds
    -40°C
    35 V
Sample Preparation
Surface Roughness: 57.83 nm
Peak to Valley: 290.77 nm

## Slide 25: NANO-INDENTATION
Neutron Irradiated
  Electropolish
    5% Perchloric acid
    95% Methanol
    5 Seconds
    -45°C
    80 V
Sample Preparation
Surface Roughness: 52.23 nm
Peak to Valley: 244.72 nm

## Slide 26: NANO-INDENTATION
Ion Irradiated
  No Polishing Performed
    Prevent loss of irradiated layer
Sample Preparation
Surface Roughness: 100.172 nm
Peak to Valley: 732.387 nm

## Slide 27: NANO-INDENTATION
Hysitron TI-950
  MaCS Lab, CAES
Depth Control
High Load Berkovich Indenter
[10]
[11]
65.3°

## Slide 28: NANO-INDENTATION
Sample Mounts
Ion Irradiated
As Received
Neutron Irradiated

## Slide 29: Experimental APPROACH
Irradiate the Samples
Perform Nano-Indentation
Determine Plastic Zone
Determine Tensile Properties

## Slide 30: PLASTIC DEFORMATION
Dislocation Imaging
Orientation Mapping
[12]
[13]

## Slide 31: PLASTIC DEFORMATION
Polycrystalline Irradiated Material
[14]

## Slide 32: PLASTIC DEFORMATION
TEM Sample Preparation
FOCUSED ION BEAM
  FEI Quanta™ 3D FEG
  MaCS Lab (CAES)
[15]

## Slide 33: PLASTIC DEFORMATION
TEM Sample Preparation
As Received
Ion Irradiated
Neutron Irradiated

## Slide 34: PLASTIC DEFORMATION
TEM Sample Preparation

## Slide 35: PLASTIC DEFORMATION
ASTAR Imaging
Image software that scans the sample and records diffraction patterns as it goes.
  Structure File
    Pearson’s Crystal Data
    Fe 92%, Cr 8%
    a = 2.877 nm
    Space Group 229
      Imm

## Slide 36: PLASTIC DEFORMATION
As Received
Neutron Irradiated
ASTAR Imaging

## Slide 37: PLASTIC DEFORMATION
As Received
Neutron Irradiated
Ion Irradiated
TEM Imaging
1 μm
1 μm
1 μm

## Slide 38: PLASTIC DEFORMATION
As Received
Neutron Irradiated
Ion Irradiated
TEM Imaging
1 μm
1 μm
1 μm

## Slide 39: PLASTIC DEFORMATION
As Received
Neutron Irradiated
Ion Irradiated
Johnson’s Model |  | 
 | Plastic Zone (μm) | Percent Difference
Ion Irradiated | 4.33 | 3.5%
Neutron Irradiated | 3.79 | 3.0%
As Received | 3.17 | 3.9%
4.181 μm
3.679 μm
3.297 μm

## Slide 40: PLASTIC DEFORMATION
As Received
Neutron Irradiated
Ion Irradiated
4.181 μm
3.679 μm
3.297 μm
4.380 μm
3.758 μm
3.129 μm

## Slide 41: PLASTIC DEFORMATION
Summary
  ASTAR imaging demonstrates non-uniform orientation between grains
  Plastic zone in polycrystalline materials can be imaged through bright field TEM.
  For 9Cr ODS ratio of plastic zone to indentation depth is:

## Slide 42: PLASTIC DEFORMATION
Summary
  ASTAR imaging demonstrates non-uniform orientation between grains
  Plastic zone in polycrystalline materials can be imaged through bright field TEM.
  For 9Cr ODS ratio of plastic zone to indentation depth is:
Ion Irradiated: 5.97x
Neutron Irradiated: 6.24x
As Received: 6.59X

## Slide 43: Experimental APPROACH
Irradiate the Samples
Perform Nano-Indentation
Determine Plastic Zone
Determine Tensile Properties

## Slide 44: TENSILE PROPERTIES
Nano-Hardness (GPa)
Indentation Depth (nm)

## Slide 45: TENSILE PROPERTIES
  Surface Effects:
Nano-Hardness (GPa)
Indentation Depth (nm)
As Received

## Slide 46: TENSILE PROPERTIES
  Surface Effects:
As Received

## Slide 47: TENSILE PROPERTIES
  Surface Effects:
As Received

## Slide 48: TENSILE PROPERTIES
  Surface Effects:
  Nano-Hardness Range:
  Elastic Modulus Range:
    4.43 – 4.99 GPa
    210.40 – 226.42 GPa
As Received
Nano-Hardness (GPa)
Indentation Depth (nm)

## Slide 49: TENSILE PROPERTIES
  Indentation Size Effect
  Nano-Hardness Range:
  Nano-Modulus Range:
    4.67 – 5.14 GPa
    216.83 – 227.51 GPa
Nano-Hardness (GPa)
Indentation Depth (nm)
Neutron Irradiated

## Slide 50: TENSILE PROPERTIES
Irradiation Hardening (GPa)
Indentation Depth (nm)
Neutron Irradiated

## Slide 51: TENSILE PROPERTIES
  Surface Effects
  Nano-Hardness Range:
  Nano-Modulus Range:
    4.31 – 5.19 GPa
    188.62 – 197.70 GPa
Nano-Hardness (GPa)
Indentation Depth (nm)
Ion Irradiated

## Slide 52: TENSILE PROPERTIES
  Irradiation Softening occurs at depths less than 500 nm
  Hardening increases until approaches neutron hardening at 700 nm
Irradiation Hardening (GPa)
Indentation Depth (nm)
Ion Irradiated

## Slide 53: TENSILE PROPERTIES
Microstructure (Swenson) |  |  |  | 
 | Ion |  | Neutron | 
 | Density (m-2) | Diameter (nm) | Density (m-2) | Diameter (nm)
Dislocation Lines | 2.04 x 1015 | - | 1.85 x 1015 | -
Carbides | 1.7 x 1019 | 0.09 | 4.7 x 1019 | 0.10
Nano-Clusters | 3.85 x 1023 | 2.20 | 4.35 x 1023 | 1.91
Voids | 4.6 x 1020 | 7.46 | 2.4 x 1020 | 3.64
Dislocation Loops | 3.1 x 1021 | 21.5 | 2.7 x 1021 | 9.5
Nano-Indentation |  | 
 | Ion | Neutron
ΔHave(MPa) | 285.03 | 262.39
Δσys (GPa) | 88.94 | 81.87
N = Number density of the obstacle (#/m3)
d = Average diameter of the obstacles (nm)
[7]
Validation of Ion Irradiated

## Slide 54: TENSILE PROPERTIES
Stress Strain Curve
[8]
[16]

## Slide 55: TENSILE PROPERTIES
Stress Strain Curve
[17]
[9]

## Slide 56: TENSILE PROPERTIES
True Stress (MPa)
True Strain
Stress Strain Curve
neutron
ion
as received
As Received | 0.205
Neutron | 0.340
Ion | 0.305
As Received | 0.205
Neutron | 0.340
Ion | 0.305

## Slide 57: TENSILE PROPERTIES
Summary
  Irradiation induced hardening is observed in both the neutron and ion irradiated samples
  Extent of hardening is consistent with microstructure
  The plastic deformation is altered by the irradiation effects, as demonstrated by the effective strain hardening coefficient

## Slide 58: CONCLUSIONS
Plastic deformation in polycrystalline materials can be characterized through TEM bright field imaging.
Irradiation induced hardening is observed in 9Cr ODS under ion irradiation at 400°C, and neutron irradiation at 500°C.
Possible ultimate tensile strength is altered by irradiation as shown by increases in the strain hardening coefficient of 49% and 39% for the neutron and ion irradiation conditions, respectively.
Indentation sample volume influences on tensile properties are more prominent in the region of plastic deformation than in the elastic region.

## Slide 59: REFERENCES
[1] M. Roser, “World Population Growth,” OurWorldINData.org, 2015. [Online]. Available: http://ourworldindata.org/data/population-growth-vital-statistics/world-population-growth/. [Accessed: 28-Jul-2015].
[1] https://atrnsuf.inl.gov/, 2015.
[2] http://www.slideshare.net/ranasajjad484/iron-carbon-dia-presentation, 2015
[3] L. Toualbi, C. Cayron, P. Olier, J. Malaplate, M. Praud, M.-H. Mathon, D. Bossu, E. Rouesne, a. Montani, R. Logé, and Y. de Carlan, “Assessment of a new fabrication route for Fe–9Cr–1W ODS cladding tubes,” J. Nucl. Mater., vol. 428, no. 1–3, pp. 47–53, Sep. 2012.
[4] R. L. Klueh and D. R. Harries, High-Chromium Ferritic and Martensitic Steels for Nuclear Applications. ASTM Int’l, 2011.
[5] A. R.R and D. Jaramillo, “Precipitation adn mechanical properties of aluminum alloys,” in Mechanical Behavior of Precipitation Hardened Aluminum Alloys Welds, Light Metal Alloys Applications, Intech, 2014.
[6] C. Race, The Modelling of Radiation Damage in Metals Using Ehrenfest Dynamics, 2011th ed. Berlin, Heidelberg: Springer Berlin Heidelberg, 2010.
[7] G.S. Was, Fundamentals of Radiation Materials Science: Metals and Alloys. 2007.
[8] P. Hosemann, D. Kiener, Y. Wang, and S. a. Maloy, “Issues to consider using nano indentation on shallow ion beam irradiated materials,” J. Nucl. Mater., vol. 425, no. 1–3, pp. 136–139, Jun. 2012.
[9] https://atrnsuf.inl.gov/, 2015
[10] https://www.hysitron.com/products-services/standalone-instruments/ti-950-triboindenter, 2015
[12] D. Hardie, S.G. Roberts, “Nanoindentation of model Fe-Cr alloys with self-ion irradiation,” Journal of Nuclear Materials, vol. 433, pp.174-179, 2013.
[13] D. Kiener, R. Pippan, C. Motz, and H. Kreuzer, “Microstructural evolution of the deformed volume beneath microindents in tungsten and copper,” Acta Mater., vol. 54, no. 10, pp. 2801–2811, 2006.
[14] B. Bose, R.J. Klassen, “Effect of ion irradiation and indentation depth on the kinetics of deformation during micro-indentation of Zr-2.5%Nb pressure tube material at 25°C,” Journal of Nuclear Materials, vol. 399, pp. 32-37, 2010.
[15] http://www.birmingham.ac.uk/facilities/electron-microscopy/microscopes/index.aspx, 2015.
[16] C. Robertson, B. K. Panigrahi, S. Kataria, Y. Serruys, M. H. Mathon, and C. S. Sundar, “Particle stability in model ODS steels irradiated up to 100 dpa at 600C: TEM and nano-indentatin investigation,” J. Nucl. Mater., vol. 426, pp. 240–246, 2012.
[17] M. Mata, O. Casals, and J. Alcalá, “The plastic zone size in indentation experiments: The analogy with the expansion of a spherical cavity,” Int. J. Solids Struct., vol. 43, no. 20, pp. 5994–6013, Oct. 2006.
[18] L.A. Giannuzzi, F.A. Stevie, “A review of focused ion beam milling techniques for TEM specimen preparation, “Micron,” vol. 30, pp. 197-204, 1999.

## Slide 60: Thank You
Corey Dolph, Research Assistant
Email: coreydolph@boisestate.edu

## Slide 61: FIB Operation
FOCUSED ION BEAM
  Operates like a SEM
    Ga+ Ion Beam
      Low melting point (85.6°F)
      Fine probe size (< 10 nm)
    Electron Beam
[18]

## Slide 62: PLASTIC DEFORMATION
Electron beam platinum deposition
  Rectangle
  5.0 kV
  3.0 nA
  z = 0.3 μm
TEM Sample Preparation

## Slide 63: PLASTIC DEFORMATION
Ion beam platinum deposition
  Rectangle
  30.0 kV
  0.5 nA
  z = 4.0 μm
TEM Sample Preparation

## Slide 64: PLASTIC DEFORMATION
Trench Cut
  Regular Cross Section
  30.0 kV
  15.0 nA
  z = 15.0 μm
TEM Sample Preparation

## Slide 65: PLASTIC DEFORMATION
Trench Cut
  Cleaning Cross Section
  30.0 kV
  7.0 nA
  z = 7.0 μm
TEM Sample Preparation

## Slide 66: PLASTIC DEFORMATION
U cuts
  Rectangle
  30.0 kV
  5.0 nA
TEM Sample Preparation

## Slide 67: PLASTIC DEFORMATION
Mount to grid
  Pt welds using Omniprobe
  30.0 kV
  50.0 pA
TEM Sample Preparation

## Slide 68: PLASTIC DEFORMATION
Thinning
  Cleaning Cross Section
  30.0 kV
  3.0 nA
  ~ 1 μm
TEM Sample Preparation

## Slide 69: PLASTIC DEFORMATION
Thinning
  Cleaning Cross Section
  30.0 kV
  1.0 nA
  ~ 500 nm
TEM Sample Preparation

## Slide 70: PLASTIC DEFORMATION
Thinning
  Cleaning Cross Section
  30.0 kV
  0.3 nA
  ~ 250 nm
TEM Sample Preparation

## Slide 71: PLASTIC DEFORMATION
Thinning
  Cleaning Cross Section
  30.0 kV
  0.1 nA
  ~ 100 nm
TEM Sample Preparation

## Slide 72: PLASTIC DEFORMATION
Final Thinning
  Rectangle
  5.0 kV
  77.0 pA
TEM Sample Preparation

## Slide 73: PLASTIC DEFORMATION
Final Thinning
  Rectangle
  2.0 kV
  48.0 pA
TEM Sample Preparation

## Slide 74: Evolution of Plastic Zone
100 nm
200 nm